## Slide 1: Scanning Microwave Microscopy:
MIM 2016
July 26, 2016
Jonathan D. Chisum
jchisum@nd.edu
Sub-surface Nano-electronic Characterization?

## Slide 2: Microscopy for Nano-characterization
 | Method |  |  | 
Parameter | Optical | STM | SEM | AFM
Contrast | reflection | Topography, chemistry | scattered e- | Topography
Region | Surface w/ depth of field | Surface | Surface w/ depth of field | Surface
Resolution | 200 nm | sub-nm | nm | nm
Duration | real time | N2 | N2 | N2
Prep. | various | planar, conductive | gold plate, vacuum | planar
Scanning Probe Microscopy
AFM is tool of choice for nano-electronics
Notes: Optical -> onion skin
STM -> clean gold surface
AFM -> Graphite
SEM -> photoresist
NFMM ->

## Slide 3: AFM for Nano-electronics
Instrument
Nano-materials and nano-devices demand nanometric electrical characterization
Material diversity (conducting, semiconducting, insulating) eliminates surface treatment (e.g., STM, SEM)
Planarity requirement of AFM is not an issue in nano-electronics
AFM is a generally a topographic measurement so flexibility must come from [1]:
  Method variants (instrument)
  Tip diversity
[1] Oliver, Rep. Prog. Phys. 71 (2008) 076501
Opensource Handbook of Nanoscience and Nanotechnology/CC-BY-2.5

## Slide 4: Nano-electronic Applications of AFM
Defect detection in boules of Si [2]
Surface roughness of wafer polishing [3]
Surface finish of etching in micromachining [4]
Photoresist characterization [5]
Oxidation [6] and metallization [7] assessment
Defect characterization in deposition [8]
[2] Nishikawa et al., Japan J. Appl. Phys. 1, 36 6595-600
[3] Abe et al., Japan J. Appl. Phys. 1 31 721-8
[4] Baum & Schiffrin, J. Micromech. Microeng. 7 338-42
[5] Huck et al., Langmuir 15 6862-2
[6] Ohmi et al., IEEE Trans. Electr. Dev. 39 537-45
[7] Chyan et al., J. Electrochem. Soc. 143 92-6
[8] Oliver et al., J. Cryst. Growth 289 506-14
[9] Saive et al., J. Adv. Funct. Mater. 2013 23, 5854
These are surface measurements. Sub-surface requires cross-sectioning via cleaving or ramps via FIB milling.

## Slide 5: AFM Variants
EFM, KPFM: Electrical Force, Kelvin Force, surface potential microscopy scans in tapping mode and measures local surface potential. Requires a topography scan and a “lift” scan to differentiate van der Waal’s forces from Coulomb forces
SCM: Scanning Capacitance uses a metal-coated tip scanned in contact-mode and measures MOS capacitor under AC bias. |dC/dV| measures carrier concentration and angle(dC/dV) determines p/n-type.
Veeco Support Note No. 289A
Park AFM Mode Note, “SCM”

## Slide 6: AFM Variants (cont’d)
C-AFM: (a.k.a, TUNA) Tunneling current through an oxide layer is measured with a linear current amplifier.
SSRM: Characterizes carrier concentration in semiconductors through spreading resistance.
SMM: Measures complex impedance (permittivity and conductivity) which permits measurement of doping and has sub-surface sensitivity w/o cross-sectioning.
1 µm
0.1µm
Si
Cu
2.25 µm
1 GHz
3 GHz
4 GHz
1.00 µm
0.87 µm
1.75 µm
f0, Q

## Slide 7: Dopant-level Characterization
Recent hardware Trojans have shown up in dopant (bottom of metal) and require no change in metallization
Top-metal is a Faraday cage
Dopant access requires backside scanning
Wafer thinning is critical but only goes so far…
Microscope photo of IBM’s Copper wiring on CU-11 ASIC 130nm technology
Need to understand scanning
at depth
Metal
N-type
P-type
Becker et al., CHES 2013

## Slide 8: Microscopy
 | Method |  |  |  | 
Parameter | Optical | STM | SEM | AFM | SMM
Contrast | reflection | Topography, chemistry | scattered e- | Topography | μ, ε, σ
Region | Surface w/ depth of field | Surface | Surface w/ depth of field | Surface | Surface, Sub-surface
Resolution | 200 nm | sub-nm | nm | nm | nm
Duration | real time | N2 | N2 | N2 | N2
Prep. | various | planar, conductive | gold plate, vacuum | planar | planar
AFM Variant
Notes: Optical -> onion skin
STM -> clean gold surface
AFM -> Graphite
SEM -> photoresist
NFMM ->

## Slide 9: Tip Modifications: SMM
CPW and Stripline cantilevers shields parasitic capacitance and efficiently delivers microwave signal
Micromachined or FIB deposited tips
Lai et al., Appl. Phys. Lett. 93, 123105 (2008)
Yang et al., J. Micromech. Microeng. 24 (2014) 045026
http://www.asylumresearch.com/Probe/SMIM150-G5,PrimeNano
PrimeNano
sMIM150-G5
Need method of assessing tip designs with complex geometries

## Slide 10: Analytical Resolution: Rectangular Aperture
ki
kr
Indistinguishable.
ki
Distinguished
(Propagating Spherical Wave)
(Decaying confined field)
Propagating
Evanescent
Notes: -- For now we will solve the problem of a uniform plane wave incident on a sub-wavelength aperture (l<<lambda) at (z=0). The uniform plane wave illuminates the aperture with a uniform distribution (rect-functions).
-- Though this solution is not our specific NFMM scenario we will show that it describes the main features of our NFMM scenario and is an analytically tractable problem.
-- We desire an expression for the E-field at every point in space (z>0). Maxwell’s equations in the source-free region (z>0) yield the source-free wave equation. However, this 2nd order PDE is not generally solvable but we can take the 2D F.T. of the E-field which reduces the 2nd order PDE to a 2nd order ODE which is solvable. The solution yields an expression for the z-dependence of the double F.T. of E. Specifically, it is an exponential decay from the aperture along the z-axis.
-- But, we did not want a solution for the F.T.{E}, rather E itself. We need only inverse F.T. the solution to find the actual E-field at any point in along the z-axis.
-- This F.T. process yields a superposition of complex exponential basis functions which are, in our case, plane waves propagating at various angles. Hence, we end up with the “angular spectrum”.

## Slide 11: Angular Spectrum at Depth
Field distribution at a point z0 can be projected through a homogenous medium to any point z1
z0=0 nm
z1=50 nm
Fourier Transform of “aperture”
wave propagation
Requires aperture distribution and homogeneous medium

## Slide 12: Image Theory
PSF

## Slide 13: SMM PSF from Full-wave Simulation
Setup: 25nm conductive tip 5nm over bulk silicon
Conical and Pyramidal tips
Cross-sectional field profiles measured versus depth in 25 nm steps
Surface profile
Conical tip
Surface profile
Pyramidal tip
x
z
x
y

## Slide 14: Field Cuts at Depth
Surface (z=0)
Sub-surface (z=-350 nm)
Evanescent field strength decays exponentially

## Slide 15: Modulation Transfer Function
|=|𝔉{PSF(r)}|
Spatial Frequency (lines/meter)
Normalized MTF (A.U.)
Depth | Conical | Pyramidal
0 nm | 15 MLines/meter (1.3 dtip) | 13 MLines/meter (1.5 dtip)
2dtip, 100 nm | 1.3 MLines/meter (15 dtip) | 1.3 MLines/meter (15 dtip)
7dtip, 350 nm | 500 kLines/meter (40 dtip) | 720 kLines/meter (28 dtip)
6dB reduction in noise floor increases max spatial frequency by 4x
Surface (z=0)
Sub-surface (z=-350 nm)
dtip=50nm

## Slide 16: Conclusions: Increasing sensitivity?
IR laser
fmod
Lock-in
fmod
Resolution is 1/10th at depth of 100nm (2dtip)
Reducing noise floor allows for sensitive detection
Modulate dopants w/ back-side IR lasers (Si is transparent to IR), possibly use cryogenic cooling
Dopant modulation
Sub-resolution steps

## Slide 17: Acknowledgements
Student: Nicholas Estes
Collaborators: Dr. Anthony Hoffman, Dr. Zoya Popovic, Dr. Suman Datta, Mr. Matthew Kay

## Slide 18: Backup

## Slide 19: Modulation Transfer Function
Edge Target
PSF
ESF
LSF
MTF
O
=
F{}
d/dx
ESF
Measure
Process
2D
1D

## Slide 20: MTF
M1/M2 scanned below 1um of SiN passivation
M0 scanned below 1um SiN passivation and 7.92 um of BCB
Resolution at depth is a questions of SNR
5.32 μm
7.92 μm
4.73 μm
10μm
10μm
50μm
M1/2
M0
M1/2
Noise floor

## Slide 21: “Super” resolution
ki
kr
Indistinguishable.
ki
Distinguished
Notes: -- For now we will solve the problem of a uniform plane wave incident on a sub-wavelength aperture (l<<lambda) at (z=0). The uniform plane wave illuminates the aperture with a uniform distribution (rect-functions).
-- Though this solution is not our specific NFMM scenario we will show that it describes the main features of our NFMM scenario and is an analytically tractable problem.
-- We desire an expression for the E-field at every point in space (z>0). Maxwell’s equations in the source-free region (z>0) yield the source-free wave equation. However, this 2nd order PDE is not generally solvable but we can take the 2D F.T. of the E-field which reduces the 2nd order PDE to a 2nd order ODE which is solvable. The solution yields an expression for the z-dependence of the double F.T. of E. Specifically, it is an exponential decay from the aperture along the z-axis.
-- But, we did not want a solution for the F.T.{E}, rather E itself. We need only inverse F.T. the solution to find the actual E-field at any point in along the z-axis.
-- This F.T. process yields a superposition of complex exponential basis functions which are, in our case, plane waves propagating at various angles. Hence, we end up with the “angular spectrum”.

## Slide 22: “Super” resolution (cont’d)
Incident
90-deg (x↔y)
Angling, Far-field
90-deg, Near-field
Propagation |  |  | Wavelength |  |  | Angle |  | 
α | γ |  | λx | λz |  | ξ |  | Comment
0 | 1 |  | ∞ | 0.3 |  | 0 |  | z-prop (ξ=0), xy-uniform
0.1 | 0.995 |  | 3 | 0.301 |  | 5.7 |  | Prop at ξ, transverse-uniform
.75 | 0.661 |  | .4 | .454 |  | 49 |  | 
1 | 0 |  | .3 | ∞ |  | 90 |  | x-prop (ξ=90), yz-uniform
1.1 | -j0.46 |  | .27 | +j0.65 |  | 90+j25 |  | x-prop, y-uniform, z-decay
5 | -j4.89 |  | .06 | +j.06 |  | 90+j131 |  | 
f0=1GHz, λ=0.3 m
X-resolution is 90-degrees, with strong evanescent decay.
k1
k3
k3

## Slide 23: Pathological Example
If the spatial correlation distance is less than the tip width unique detection is possible.
C = C0*(7/10)+C0’*(3/10)
C = C0*(7/10)+C0’*(3/10)
C = C0*(8/10)+C0’*(2/10)